## Slide 1
GLOBAL AI + MATERIALS INNOVATION COMPETITION 2026
SecureCoating-Vision
Multi-Sensor AI for Inline Battery-Electrode Inspection
多传感器 AI 在线电极检测与闭环诊断平台
Team 71 • Trịnh Hoàng Tú, HUFLIT
Academic Advisor: Prof. Kris Singh — CEO SRII, Visiting Prof. Tsinghua University
TRACK 4
AI + MATERIALS TESTING
AND CHARACTERIZATION
人工智能 + 材料检测与表征
Decision objective: prove a defensible inline inspection architecture — not a dashboard demo.
0:00–0:35 | Opening thesis
TEAM 71 / 1
Notes: Good morning, distinguished judges. I am Trịnh Hoàng Tú from Team 71.
SecureCoating-Vision is designed as an inline decision system: it converts physical sensing into a timestamped, spatially traceable quality action. Our contribution is not another vision demo. It is the engineering bridge from photons on a moving electrode to a guarded factory decision.
In six minutes, I will show the physical budget, the multi-modal timing anchor, the measurement guard bands, and the deployment gate we use before claiming production readiness.
[Sources]
Project identity and team details supplied by Team 71.

## Slide 2
02 | 0:35–1:15
The defect is tiny; the consequence is not
微小缺陷，巨大后果
PROTOTYPE VISUAL — SYNTHETIC DATA
SEPARATOR REFERENCE
14 µm
Risk boundary for stack design
INSPECTION GAP
Subsurface
Surface-only RGB cannot see void physics
Factory consequence
A defect escape is not “one missed box.”
It is an untraceable precursor to rework, yield loss, or an internal-short investigation.
The engineering question: can we detect, measure, locate, and act before slitting?
Problem framing; the illustrated sample is procedurally generated.
TEAM 71 / 2
Notes: A gigafactory does not fail because it cannot draw a bounding box. It fails when a critical electrode defect travels downstream without a reliable location, a physical measurement, or a disposition.
The separator reference is 14 micrometres in the configured cell-stack model. That is a risk-design reference, not a universal threshold. Surface-only inspection misses hidden thermal and topographic signatures. Our task is to bring those signals into one coordinate system and make the reject decision traceable.
[Sources]
Prototype image: data/test_set/images/defect_val_00000.jpg (procedurally generated). Separator reference: src/inference/electrode_metrology.py.

## Slide 3
03 | 1:15–2:00
Seven stages, one physically closed inspection decision
七工站闭环检测决策
1
Encoder
同步
2
RGB / Thermal / 3D
采集
3
5-channel
对齐融合
4
AI segmentation
推理
5
Physics
metrology
6
PLC
interlock
7
Root-cause
feedback
WEB SPEED
1.8 m/s
design operating point
LINE RATE
42.6 kHz
1.8 m/s ÷ 42.24 µm/px
OPTICS
M = 0.17
2 × 8K line-scan
MOTION BLUR
≤ 0.40 px
exposure design limit
Optical budget is a calculable requirement — not a marketing number.
Design budget: 50 mm lens, 350 mm WD, 7.04 µm sensor pixels, 650 mm web.
TEAM 71 / 3
Notes: This is the system architecture. It starts with the encoder because coordinates matter before AI matters. Two 8K line-scan cameras cover the web; thermal and height channels add material physics; inference produces a mask; metrology turns the mask into a measured event; the interlock schedules an action; and the digital twin connects defects to upstream process hypotheses.
The key proof point is the optical budget. With magnification 0.17 and 42.24 micrometres per object-space pixel, 1.8 metres per second requires 42.6 kilohertz line rate. The exposure limit is set to stay under 0.4 pixels of blur. These are engineering calculations that must be bench-verified with the selected camera and illumination.
[Sources]
src/industrial/optical_budget.py.

## Slide 4
04 | 2:00–2:45
Fusion is anchored to material coordinates, not arrival time
多模态融合：锚定材料坐标，而非到达时间
FrameContext
roll ID
encoder pulse at capture
monotonic timestamp
RGB
surface texture
Traveling-wave thermal
phase / subsurface response
Laser 3D
height / topology
5-layer tensor
[R, G, B, ΔT/phase, Z]
spatial warp + quality flags
Decision event
X_m · Y_mm · lane
confidence · disposition
FrameContext preserves the web position at photon capture; downstream latency cannot shift the defect coordinate.
Temporal anchoring is implemented in the prototype; real sensor streams remain a pilot integration gate.
TEAM 71 / 4
Notes: Multi-modal fusion fails if it uses processing time as a coordinate. Our FrameContext records the roll ID, encoder count, material position and monotonic capture time when the photons arrive. Every later operation inherits that anchor.
We fuse RGB, traveling-wave thermal response, and 3D laser height into five channels: R, G, B, thermal phase or differential, and height. Importantly, the current repository validates this logic with simulated secondary streams. The production claim is therefore the architecture and anchoring method; hardware calibration and temporal phase validation are pilot gates.
[Sources]
src/industrial/web_synchronizer.py; src/inference/sensor_fusion.py (mock/simulated secondary feeds).

## Slide 5
05 | 2:45–3:35
A mask becomes a guard-banded measurement record
从分割掩膜到带防护带的测量记录
1 Geometry
minAreaRect · web angle · area
2 Topography
plane leveling · Ra · volume
3 Risk index
separator-aware empirical score
4 Guard band
limit − expanded uncertainty U
5 Traceability
plant SOP / customer spec mapping
UNCERTAINTY
GUM k = 2
expanded uncertainty; 95% coverage
DECISION RULE
Limit − U
guard band before A/B/C grade
Standards correction: T/CIAPS 0006 and QC/T 743 are not valid coating-metrology compliance claims.
Use plant-approved acceptance limits and an ISO 17025/GUM validation plan before compliance language.
TEAM 71 / 5
Notes: We do not stop at segmentation. We calculate geometry from minAreaRect, level the local 3D baseline, estimate topographic measures, and attach an expanded uncertainty using a GUM-style k equals two budget. The disposition uses a guard band: the decision limit is tightened by uncertainty before assigning Grade A, B, or C.
There is a standards correction that must remain in the final deck. T/CIAPS 0006 is a PCS–BMS CAN protocol, and QC/T 743-2006 is abolished. They cannot be presented as electrode inspection compliance. In production, each limit must be mapped to an approved plant SOP, customer specification, or applicable current standard.
[Sources]
src/inference/electrode_metrology.py; national standards platform (QC/T 743-2006 status); T/CIAPS 0006-2020 scope.

## Slide 6
06 | 3:35–4:20
Latency is a full physical chain — and currently a design model
时延是完整物理链路——当前为设计模型
Tile formation
12.1 ms
+
DMA
1.2 ms
+
Fusion
1.8 ms
+
AI
8.7 ms
+
Metrology
1.5 ms
+
Network
0.8 ms
+
PLC
2.0 ms
+
Valve + air
4.5 ms
P50 DESIGN MODEL
32.9 ms
not a hardware measurement
P99.9 MODEL
35.9 ms
Monte Carlo output
DESIGN W/ GUARD
38.9 ms
P99.9 + 3.0 ms
500 mm BUFFER
7.1×
at 1.8 m/s; design result
PLC protocol telemetry ≠ deterministic safety interlock. HIL evidence is mandatory before deployment.
Latency engine status in source: MONTE_CARLO_SIMULATED; the P99.9 number is not a measured production SLA.
TEAM 71 / 6
Notes: A fast neural network is not a fast rejection system. We decompose the chain from tile formation to air-jet propagation. The expected P50 is 32.9 milliseconds, P99.9 is 35.9 milliseconds, and with a three-millisecond guard the design latency is 38.9 milliseconds. At 1.8 metres per second and 500 millimetres camera-to-ejector spacing, that gives a 7.1-times design buffer.
However, these percentiles are Monte Carlo modeled in the current code. Modbus TCP and OPC UA are telemetry/control interfaces, not proof of a deterministic safety layer. The pilot exit criterion is a hardware-in-the-loop trace with encoder, PLC scan, valve response and P99.9 measurement.
[Sources]
src/industrial/latency_budget.py (Monte Carlo status); calculated 500 / (1.8 × 0.0389).

## Slide 7
07 | 4:20–5:10
Defects become controlled process experiments
将缺陷转化为受控工艺实验
1,200 m roll map
X_m · Y_mm
4 slitting lanes
quality events
Root-cause rank
Slot-die · Dryer Z1
Vacuum mixer
Constrained change
ΔT1 / Δv / ΔQ
approval + recipe limits
Verify effect
holdout segment
roll-level evidence
PROTOTYPE CERTIFICATE
HMAC-SHA256
tamper-evident MAC; not non-repudiation
EXAMPLE INTERVENTION
ΔT1 = −4 °C
hypothesis to be confirmed by trial
REPORTED KPI
−84.2% scrap
hold claim until raw pilot evidence is supplied
Closed-loop claims require controlled intervention, approval guardrails, and before/after raw logs.
TEAM 71 / 7
Notes: The digital twin is a map of the material, not a dashboard screenshot. Each event is located by machine direction, transverse position and slitting lane. The diagnostic engine then ranks process hypotheses.
We make an important causal distinction: a correlation is not a root cause. For example, reducing Dryer Zone 1 by four degrees is a controlled hypothesis, not an autonomous action. It must be constrained by the recipe, approved by process engineering, and verified on a holdout segment. The reported 84.2 percent scrap reduction must not be spoken as a result until raw pilot logs, baseline definition and independent roll evidence are available.
[Sources]
src/industrial/web_synchronizer.py; src/traceability/root_cause_engine.py; src/traceability/roll_certificate.py; reported figure appears only in generated dossier.

## Slide 8
08 | 5:10–6:00
Pilot readiness must be earned by evidence
试点就绪性靠证据获得，而非包装宣称
PROVEN NOW
42 authored unit-test methods
full suite blocked in current runtime by missing dependencies
DESIGN-PROVEN
1.8 m/s optical budget
42.6 kHz · M=0.17 · ≤0.40 px
PILOT GATES
hardware streams + HIL + raw-roll labels
cross-lot POD · P99.9 trace · MSA/Gage R&R
DO NOT CLAIM YET
6,000 m · 0.02 ppm · −84.2%
requires raw evidence, CI, independent witness
Our ask: approve a supervised pilot to convert a defensible architecture into production evidence.
Close: evidence discipline is the competitive advantage.
TEAM 71 / 8
Notes: Our closing position is simple: SecureCoating-Vision has an engineering architecture that is worth piloting, not a production claim that should be taken on faith.
We have authored 42 unit-test methods and a coherent optical design budget. The next proof must be real sensor streams, HIL timing, measurement-system analysis, and cross-lot probability of detection. We will not claim six thousand metres, 0.02 parts per million escape, or 84.2 percent scrap reduction without raw logs and independent evidence.
That discipline is exactly why we ask for a supervised pilot. It is the fastest route from credible DeepTech prototype to deployable quality system.
[Sources]
tests/ (42 authored test methods); runtime test attempt recorded 2026-08-16; repository simulation markers and generated dossier.